Material Specification

Customer: IEWC

TOL Part Number:		GPT-10-1003

Spec Revision Level:		A6

Customer Part Number:	GPTM10T-1-P

Description:	10 GA GPT, 105 DEGC ,19 STRANDS TINNED COPPER, MARINE WIRE WITH PRINT

Conductor (Stranding):	19 X .0224” Tinned Copper

Conductor OD 		0.110 inches

Max. Lay Length:		2.0 inch

Nom. Wall Thickness:	0.031 inches

Max . O.D.                              0.185 inches

## Nom. O. D:			0.173 inches

## Min   O. D:			0.170 inches

## Max Runout:	0.008 inches

## Circular Mils (CMA):	9343 (Min)

## Surface Print:   	GPT 10 GA MARINE WIRE SAE J378 & J1128 60V DC 105C DRY

## This Product is RoHS Compliant.

# Specification Reference Data

## SAE:	J-1128 / J378			       Ford: N/A 			Chrysler: N/A

UL :  N/A			       CSA:  N/A			Packard: N/A

Other:	N/A

Therm-O-Link, Inc. certifies that the above specifications are met or exceeded in the production of this product.

Verified By:			Mir Hussain (Corporate Product Engineering Manager)

Date:	7-22-2021